AQUA GOLD

Aqua Gold HD

- Single component self - crosslinking PU system

- Extreme  scratch,  wear and chemical resistances

- Excellent levelling and brush drag properties

- Low VOC formulation

- No additional crosslinker required

TYPICAL PROPERTIES

Appearance					Milky white, translucent

Solids						30%

Density					0.96

Viscosity					110cPs @ 25°C

Volatile Organic Content Wt %		12%

APPLICATION PROPERTIES

Recoat time					6 hrs @ 25°C

Coverage					10²m/L

Gloss Level 60° Specular			Gloss 90, Satin 45, Matt 25

Wash up					Water

Full Cure					5-7 days